## Slide 1
rCB,
What is it really?
30th May 2018

## Slide 2
What is Carbon Black?

## Slide 3
Carbon Black Classification
Example = N330
Normal or Slow Cure
Indicates primary particle size
Arbitrarily assigned

## Slide 4
What is rCB?

## Slide 5
rCB Production – Pyrolysis
Simplified version!
Feedstock preparation
Pyrolysis
Particle size reduction
Pelletisation

## Slide 6
rCB Composition
*Volatiles: Controlled by Stages 1 & 2
*Carbon: Controlled by Stages 1 & 2
Ash: Controlled by Stage 1
rCB

## Slide 7
rCB Production – Feedstock (Stage 1)

## Slide 8
rCB Production – Pyrolysis (Stage 2)
Notes: Formation of carbonaceous residue
Target very low volatiles content & certainly no residual polymer

## Slide 9
rCB Production – Polishing (Stage 3)

## Slide 10
White Compound Pyrolysis
Model tread formulation prepared without the inclusion of carbon black
Shredded <5mm
Pyrolysed at 550°C

## Slide 11
White Compound Pyrolysis
4.2% Carbon from polymer decomposition

## Slide 12
rCB Colloidal Properties

## Slide 13
rCB Colloidal Properties
We’ve all seen this chart!
This is very misleading.
*rCB Performance
Window
*typical rCB
Notes: By definition, grades have narrow particle size and aggregate size distribution

## Slide 14
rCB – How does it compare to its constituents?
Blend 1: Contains N234/ N330/ N375/ N326/ N550/ N660/ N683/ N772 at ratios expected in a tyre feedstock.
Blend 2: Carbon black blend + 13% silica + 5% zinc oxide (close match to Euro rCB)
Notes: Based solely on the colloidal characteristics of the samples, we would expect the in-rubber performance of the rCB and blend 2 to fall between that of N326→N330, with blend 1 being slightly less reinforcing.

## Slide 15
ASTM D3192 – Relative IRB8 (N330)
Same trends for hardness, tensile strength….
Drop in predicted performance due to vastly broadened aggregate size distribution
Trend verified in ASTM D3191 (SBR)
Blend 1, 2 & rCB Predicted
Less
reinforcing
Notes: blend 1, which contains carbon blacks only, the reduction in reinforcing potential must be an artefact of the very wide aggregate size distribution. It is also interesting to note that the rCB sample was more reinforcing than the compositionally similar blend 2

## Slide 16
rCB Colloidal Properties
This is wrong
*typical rCB
Notes: By definition, grades have narrow particle size and aggregate size distribution

## Slide 17
rCB Colloidal Properties
This is more representative!
rCB
Notes: By definition, grades have narrow particle size and aggregate size distribution
We must find a better test to represent this as part of ASTM D36

## Slide 18
rCB Colloidal Properties
Notes: Demonstration of broad particle and aggregate size distribution

## Slide 19
Conclusion = rCB Actually Outperforms Raw Constituents

## Slide 21
Chris Norris PhD, MSc, BSc (Hons)
chris.norris@artis.uk.com
01225 896505
www.sustainable-materials-group.com
www.artis.uk.com
Thank You!
Questions?